## Lecture1.5

## The properties of p–n junction

### Electrostatic properties of p-n junction

### Junction capacitance

### Varicap or varactor diodes

## Parametric amplifiers

## The properties of p–n junction

A p–n junction is a junction formed by joining p-type and n-type semiconductors together in very close contact. The term junction refers to the boundary interface where the two regions of the semiconductor meet. Although they can be constructed of two separate pieces, p–n junctions are more often created in a single crystal of semiconductor by doping, for example by ion implantation, diffusion of dopants, or by epitaxy (growing a layer of crystal doped with one type of dopant on top of a layer of crystal doped with another type of dopant).

P-N junctions are elementary "building blocks" of almost all semiconductor electronic devices such as diodes, transistors, solar cells, LEDs, and integrated circuits; they are the active sites where the electronic action of the device takes place. For example, a common type of transistor, the bipolar junction transistor, consists of two p–n junctions in series, in the form n–p–n or p–n–p.

The discovery of the p–n junction is usually attributed to American physicist Russell Ohl of Bell Laboratories

The p–n junction possesses some interesting properties which have useful applications in modern electronics. A p-doped semiconductor is relatively conductive. The same is true of an n-doped semiconductor, but the junction between them is a nonconductor. This nonconducting layer, called the depletion zone, occurs because the electrical charge carriers in doped n-type and p-type silicon (electrons and holes, respectively) attract and eliminate each other in a process called recombination. By manipulating this non-conductive layer, p–n junctions are commonly used as diodes: circuit elements that allow a flow of electricity in one direction but not in the other (opposite) direction. This property is explained in terms of forward bias and reverse bias, where the term bias refers to an application of electric voltage to the p–n junction.

Equilibrium (zero bias)

In a p–n junction, without an external applied voltage, an equilibrium condition is reached in which a potential difference is formed across the junction. This potential difference is called built-in potential Vbi.

After joining p-type and n-type semiconductors, electrons near the p–n interface tend to diffuse into the p region. As electrons diffuse, they leave positively charged ions (donors) in the n region. Similarly, holes near the p–n interface begin to diffuse into the n-type region leaving fixed ions (acceptors) with negative charge. The regions nearby the p–n interfaces lose their neutrality and become charged, forming the space charge region or depletion layer (see figure 1).

### Figure 1. A p–n junction in thermal equilibrium with zero bias voltage applied. Electrons and holes concentration are reported respectively with blue and red lines. Gray regions are charge neutral. Light red zone is positively charged. Light blue zone is negatively charged. The electric field is shown on the bottom, the electrostatic force on electrons and holes and the direction in which the diffusion tends to move electrons and holes.

The electric field created by the space charge region opposes the diffusion process for both electrons and holes. There are two concurrent phenomena: the diffusion process that tends to generate more space charge, and the electric field generated by the space charge that tends to counteract the diffusion. The carrier concentration profile at equilibrium is shown in figure 1 with blue and red lines. Also shown are the two counterbalancing phenomena that establish equilibrium.

### Figure 2. A p–n junction in thermal equilibrium with zero bias voltage applied. Under the junction, plots for the charge density, the electric field and the voltage are reported.

The space charge region is a zone with a net charge provided by the fixed ions (donors or acceptors) that have been left uncovered by majority carrier diffusion. When equilibrium is reached, the charge density is approximated by the displayed step function. In fact, the region is completely depleted of majority carriers (leaving a charge density equal to the net doping level), and the edge between the space charge region and the neutral region is quite sharp (see figure 2). The space charge region has the same charge on both sides of the p–n interfaces, thus it extends farther on the less doped side (the n side in figures 1 and 2).

### Forward bias

Forward bias occurs when the P-type semiconductor material is connected to the positive terminal of a battery and the N-type semiconductor material is connected to the negative terminal, as shown below. This usually makes the p–n junction conduct.

### Figure 3. PN junction operation in forward bias mode showing reducing depletion width. Both p and n junctions are doped at a 1e15/cm3 doping level, leading to built-in potential of ~0.59V. Reducing depletion width can be inferred from the shrinking charge profile, as fewer dopants are exposed with increasing forward bias.

With a battery connected this way, the holes in the P-type region and the electrons in the N-type region are pushed towards the junction. This reduces the width of the depletion zone. The positive charge applied to the P-type material repels the holes, while the negative charge applied to the N-type material repels the electrons. As electrons and holes are pushed towards the junction, the distance between them decreases. This lowers the barrier in potential. With increasing forward-bias voltage, the depletion zone eventually becomes thin enough that the zone's electric field can't counteract charge carrier motion across the p–n junction, consequently reducing electrical resistance. The electrons which cross the p–n junction into the P-type material (or holes which cross into the N-type material) will diffuse in the near-neutral region. Therefore, the amount of minority diffusion in the near-neutral zones determines the amount of current that may flow through the diode.

Only majority carriers (electrons in N-type material or holes in P-type) can flow through a semiconductor for a macroscopic length. With this in mind, consider the flow of electrons across the junction. The forward bias causes a force on the electrons pushing them from the N side toward the P side. With forward bias, the depletion region is narrow enough that electrons can cross the junction and inject into the P-type material. However, they do not continue to flow through the P-type material indefinitely, because it is energetically favorable for them to recombine with holes. The average length an electron travels through the P-type material before recombining is called the diffusion length, and it is typically on the order of microns.[2]

Although the electrons penetrate only a short distance into the P-type material, the electric current continues uninterrupted, because holes (the majority carriers) begin to flow in the opposite direction. The total current (the sum of the electron and hole currents) is constant in space, because any variation would cause charge buildup over time (this is Kirchhoff's current law). The flow of holes from the P-type region into the N-type region is exactly analogous to the flow of electrons from N to P (electrons and holes swap roles and the signs of all currents and voltages are reversed).

Therefore, the macroscopic picture of the current flow through the diode involves electrons flowing through the N-type region toward the junction, holes flowing through the P-type region in the opposite direction toward the junction, and the two species of carriers constantly recombining in the vicinity of the junction. The electrons and holes travel in opposite directions, but they also have opposite charges, so the overall current is in the same direction on both sides of the diode, as required.

The Shockley diode equation models the forward-bias operational characteristics of a p–n junction outside the avalanche (reverse-biased conducting) region.

### Reverse bias

A silicon p–n junction in reverse bias.

Reverse biased usually refers to how a diode is used in a circuit. If a diode is reverse biased, the voltage at the cathode is higher than that at the anode. Therefore, no current will flow until the diode breaks down. Connecting the P-type region to the negative terminal of the battery and the N-type region to the positive terminal, corresponds to reverse bias. The connections are illustrated in the following diagram:

Because the p-type material is now connected to the negative terminal of the power supply, the 'holes' in the P-type material are pulled away from the junction, causing the width of the depletion zone to increase. Similarly, because the N-type region is connected to the positive terminal, the electrons will also be pulled away from the junction. Therefore the depletion region widens, and does so increasingly with increasing reverse-bias voltage. This increases the voltage barrier causing a high resistance to the flow of charge carriers thus allowing minimal electric current to cross the p–n junction.

The strength of the depletion zone electric field increases as the reverse-bias voltage increases. Once the electric field intensity increases beyond a critical level, the p–n junction depletion zone breaks-down and current begins to flow, usually by either the Zener or avalanche breakdown processes. Both of these breakdown processes are non-destructive and are reversible, so long as the amount of current flowing does not reach levels that cause the semiconductor material to overheat and cause thermal damage.

This effect is used to one's advantage in zener diode regulator circuits. Zener diodes have a certain - low - breakdown voltage. A standard value for breakdown voltage is for instance 5.6V. This means that the voltage at the cathode can never be more than 5.6V higher than the voltage at the anode, because the diode will break down - and therefore conduct - if the voltage gets any higher. This effectively regulates the voltage over the diode.

Another application where reverse biased diodes are used is in Varicap diodes. The width of the depletion zone of any diode changes with voltage applied. This varies the capacitance of the diode. For more information, refer to the Varicap article.

### Electrostatic properties of p-n junction

For a p-n junction Poisson's equation becomes

where is the electric potential, ρ is the charge density,  is permittivity and q is the magnitude of the electron charge.

Since the total charge on either side of the depletion region must cancel out it is

From the above equations and by deploying basic calculus it can be shown that the total width of the depletion region is

Furthermore, by implementing the Einstein relation and assuming the semiconductor is nondegenerate (i.e. the product p0n0 is independent of the Fermi energy) it follows that

where T is the temperature of the semiconductor and k is Boltzmann constant.

### Junction capacitance

In the case of the reverse biasing an abrupt pn junction can be modelled as a parallel-plate capacitor. The thickness of depletion layer (the thickness of the dielectric) is given by

,				(7.1)

where dn and dp – thickness of depletion layers on the n and p sides of the junction correspondingly, – dielectric permittivity, q – hole’s charge, UB – built-in potential, UR – reverse voltage, NA and ND – doping concentrations on the p and n sides of the junction.

The depletion capacitance Cb is given by

,					(7.2)

here S is cross-section area of the junction.

So the depletion capacitance is dependent on the junction area, reverse voltage, doping concentrations and parameters of the semiconductor.

At forward bias, electrons are injected into p region, holes are injected into n region and space charges appear. These charges are dependent on the voltage applied to the junction and storage or diffusion capacitance of the junction exists.

The diffusion capacitance is given by

,								(7.3)

here k is Boltzmann’s constant, T – temperature, ID – diffusion current,  – mean carrier life-time.

Thus, the diffusion capacitance is directly proportional to the forward junction current  and carrier life-time.

The total capacitance of a p-n junction is sum of and :

(7.4)

Under forward bias conditions the value of the depletion capacitance is small compared to . So, .

In the reverse biased pn junction the diffusion current is small. Then we have . Thus, .

### Varicap or varactor diodes

### Varicap schematic symbol

### In electronics, a varicap diode, varactor diode, variable capacitance diode, variable reactance diode or tuning diode is a type of diode which has a variable capacitance that is a function of the voltage impressed on its terminals.

### Varactors are principally used as a voltage-controlled capacitor, rather than as rectifiers. They are commonly used in parametric amplifiers, parametric oscillators and voltage-controlled oscillators as part of phase-locked loops and frequency synthesizers.

## Operation

Operation of a varicap

Varactors are operated reverse-biased so no current flows, but since the thickness of thedepletion zone varies with the applied bias voltage, the capacitance of the diode can be made to vary. Generally, the depletion region thickness is proportional to the square root of the applied voltage; and capacitance is inversely proportional to the depletion region thickness. Thus, the capacitance is inversely proportional to the square root of applied voltage.

All diodes exhibit this phenomenon to some degree, but specially made varactor diodes exploit the effect to boost the capacitance and variability range achieved - most diode fabrication attempts to achieve the opposite.

In the figure we can see an example of a cros-section of a varactor with the depletion layer formed of a p-n-junction. But the depletion layer can also be made of a MOS-diode or a Schottky diode. This is of big importance in CMOS and MMIC technology.

## Parametric amplifiers

A parametric amplifier is implemented as a mixer. The mixer's gain shows up in the output as amplifier gain. The input weak signal is mixed with a strong local oscillator signal, and the resultant strong output is used in the ensuing receiver stages.

Parametric amplifiers also operate by changing a parameter of the amplifier. Intuitively, this can be understood as follows, for a variable capacitor based amplifier.

Q [charge in a capacitor] = C x V
therefore
V [voltage across a capacitor] = Q/C

Knowing the above, if a capacitor is charged until its voltage equals the sampled voltage of an incoming weak signal, and if the capacitor's capacitance is then reduced (say, by manually moving the plates further apart), then the voltage across the capacitor will increase. In this way, the voltage of the weak signal is amplified.

If the capacitor is a varicap diode, then the 'moving the plates' can be done simply by applying time-varying DC voltage to the varicap diode. This driving voltage usually comes from another oscillator — sometimes called a "pump".

The resulting output signal contains frequencies that are the sum and difference of the input signal (f1) and the pump signal (f2): (f1 + f2) and (f1 - f2).

A practical parametric oscillator needs the following connections: one for the "common" or "ground", one to feed the pump, one to retrieve the output, and maybe a fourth one for biasing. A parametric amplifier needs a fifth port to input the signal being amplified. Since a varactor diode has only two connections, it can only be a part of an LC network with four eigenvectors with nodes at the connections. This can be implemented as a transimpedance amplifier, a traveling wave amplifier or by means of a circulator.

The parametric oscillator equation can be extended by adding an external driving force E(t):

We assume that the damping D is sufficiently strong that, in the absence of the driving force E, the amplitude of the parametric oscillations does not diverge, i.e., that αt < D. In this situation, the parametric pumping acts to lower the effective damping in the system. For illustration, let the damping be constant β(t) = ω0b and assume that the external driving force is at the mean resonance frequency ω0, i.e., E(t) = E0sinω0t.

The equation becomes

whose solution is roughly

As h0 approaches the threshold 2b, the amplitude diverges. When , the system enters parametric resonance and the amplitude begins to grow exponentially, even in the absence of a driving force E(t).

A variable capacitance diode is known as a varicap diode or as a varactor. If a diode is reverse biased, an insulating depletion region forms between the two semiconductive layers. In many diodes the width of the depletion region may be changed by varying the reverse bias. This varies the capacitance. This effect is accentuated in varicap diodes. The schematic symbols is shown in Figure below, one of which is packaged as common cathode dual diode.

Varicap diode: Capacitance varies with reverse bias. This varies the frequency of a resonant network.

If a varicap diode is part of a resonant circuit as in Figure above, the frequency my be varied with a control voltage, Vcontrol. A large capacitance, low Xc, in series with the varicap prevents Vcontrol from being shorted out by inductor L. As long as the series capacitor is large, it has minimal effect on the frequency of resonant circuit. Coptional may be used to set the center resonant frequency. Vcontrol can then vary the frequency about this point. Note that the required active circuitry to make the resonant network oscillate is not shown. For an example of a varicap diode tuned AM radio receiver see “electronic varicap diode tuning,” Ch 9

Some varicap diodes may be referred to as abrupt, hyperabrupt, or super hyper abrupt. These refer to the change in junction capacitance with changing reverse bias as being abrupt or hyper-abrupt, or super hyperabrupt. These diodes offer a relatively large change in capacitance. This is useful when oscillators or filters are swept over a large frequency range. Varying the bias of abrupt varicaps over the rated limits, changes capacitance by a 4:1 ratio, hyperabrupt by 10:1, super hyperabrupt by 20:1.

Varactor diodes may be used in frequency multiplier circuits. See “Practical analog semiconductor circuits,” Varactor multiplier

### Additional materials

### Varactor or Tuning Diodes

These types of diodes work on the principle that all diodes exhibit some capacitance. Indeed the zener diode BZX79C12 quoted above has, according to the data book, a capacitance of 65-85 pF at 0V and measured at 1 Mhz.

For AM Radio band applications a specific diode has been devised. The Philips BB212 in a TO-92 case is one such type. Each of the diodes has a capacitance of 500 - 620 pF at a reverse bias of 0.5V and <22 pF at 8V. This diode's capacitance ratio is quoted at 22.5:1 which could not be achieved easily if at all with an air variable capacitor. This type of diode is depicted in figure 1 above.

Several obvious advantages come immediately to mind, a small transistor type package, very low cost, ease of construction on a circuit board, can be mounted away from heat generating devices, frequency determining circuitry entirely dependent upon resistor values and ratios, DC voltage control can be either from frequency synthesiser circuits or perhaps a multi-turn potentiometer. Such a potentiometer aids band spreading and fine tuning if two potentiometers are used. The only real limitation is your imagination and the calculations involved.

Capacitance exists between the terminals of a transistor. The collector-base capacitance CCB and emitter-base capacitance CEB decrease the gain of a common emitter circuit at higher frequencies.

In a common emitter amplifier, the capacitive feedback from collector to base effectively multiplies CCB by β. The amount of negative gain-reducing feedback is related to both current gain, and amount of collector-base capacitance. This is known as the Miller effect, Miller effect.

## 4.5.1 Introduction

Any variation of the charge within a p-n diode with an applied voltage variation yields a capacitance which must be added to the circuit model of a p-n diode. The capacitance associated with the charge variation in the depletion layer is called the junction capacitance, while the capacitance associated with the excess carriers in the quasi-neutral region is called the diffusion capacitance.

Both types of capacitances are non-linear so that we will derive the small-signal capacitance in each case. We will find that the junction capacitance dominates for reverse-biased diodes, while the diffusion capacitance dominates in strongly forward-biased diodes. The total capacitance is the sum of both.

Expressions for the capacitances are obtained by calculating the change in charge for a change in applied voltage, or:

(pn19)

## 4.5.2 The junction capacitance

The junction capacitance is calculated using the expression for the parallel plate capacitance. This might at first seem unexpected since the charge is distributed throughout the depletion layer. However, when applying small voltage variations one finds that charge is only added and removed at the edge of the depletion region so that the capacitance simply depends on the dielectric constant, the area and the depletion layer width, yielding:

(pn14)

where the depletion layer width, w, was obtained from the electrostatic analysis.

## 4.5.3 The diffusion capacitance

## 4.5.4 Capacitance measurement and parameter extraction

A capacitance versus voltage measurement can be used to obtain the built-in voltage and the doping density of a one-sided p-n diode. Plotting one over the capacitance squared one expects a linear dependence as expressed by:

(pn15)

A calculated capacitance-voltage and corresponding 1/C2 curve is shown in the figure below:

pncap.xls - pncap.gif

Fig. 4.5.1 Capacitance and 1/C2 versus voltage of a p-n diode with Na = 1016 cm-3, Nd = 1017 cm-3 and an area of 10-4 cm2

The built-in voltage is obtained at the intersection of the 1/C2 curve and the horizontal axis, while the doping density is obtained from the slope of the curve. A capacitance-voltage measurements also provides the doping density profile of one-sided p-n diodes. For a p+-n diode one obtains the doping density from:

(pn16)

while the depth equals the depletion layer width which is obtained from w = sA/Cj. Both the doping density and the corresponding depth can be obtained at each voltage yielding a doping profile.