Si

Properties of Si

| Atoms/cm3 | 5.0E22 |
| --- | --- |
| Atomic Weight | 28.09 |
| Breakdown field (V/cm) | ~3E5 |
| Crystal structure | Diamond |
| ensity (g/cm3) | 2.328 |
| Dielectic Constant | 11.9 |
| Nc (cm-3) | 2.8E19 |
| Nv (cm-3) | 1.04E19 |
| Effective Mass, m*/m0 Electrons m*l m*l Holes m*eh m*hh | 0.98 0.19 0.16 0.49 |
| Electron affinity, x(V) | 4.05 |
| Energy gap (eV) at 300K | 1.12 |
| Intrinisic carrier conc. (cm-3) | 1.45E10 |
| Intrinsic Debye Length (um) | 24 |
| Intrinsic resistivity (-cm) | 2.3E5 |
| Lattice constant (A) | 5.43095 |
| Linear coefficient of thermal expansion, L/LT(C-1) | 2.6E-6 |
| Melting point (C) | 1415 |
| Minority carrier lifetime (s) | 2.5E-3 |
| Mobility (drift) (cm2/V-8) | 1500 450 |
| Optical-phonon energy (eV) | 0.063 |
| Phonon mean free path (A) | 76(electron) 55(hole) |
| Specific heat (J/g C) | 0.7 |
| Thermal conductivity (W/cmC) | 1.5 |
| Thermal diffusivity (cm2/s) | 0.9 |
| Vapor pressure (Pa) | 1 at 1650C 1E-6 at 900 C |

GaAs

Properties of GaAs

| Atoms/cm3 | 4.42E22 |
| --- | --- |
| Atomic Weight | 144.63 |
| Breakdown field (V/cm) | ~4E5 |
| Crystal structure | Zincblende |
| Density (g/cm3) | 5.32 |
| Dielectic Constant | 13.1 |
| Nc (cm-3) | 4.7E17 |
| Nv (cm-3) | 7.0E18 |
| Effective Mass, m*/m0 Electrons Holes m*lh m*hh | 0.067 0.08 0.45 |
| Electron affinity, (V) | 4.07 |
| Energy gap (eV) at 300K | 1.424 |
| Intrinisic carrier conc. (cm-3) | 1.79E6 |
| Intrinsic Debye length (um) | 2250 |
| Intrinsic resistivity (-cm) | 1E8 |
| Lattice constant (A) | 5.6533 |
| Linear coefficient of thermal expansion, L/(L T) (C-1) | 6.86E-6 |
| Melting point (C) | 1238 |
| Minority carrier lifetime (s) | ~1E-8 |
| Mobility (drift) (cm2/V-s) | 8500 400 |
| Optical-phonon energy (eV) | 0.035 |
| Phonon mean free path (A) | 58 |
| Specific heat (J/g C) | 0.35 |
| Thermal conductivity (W/cmC) | 0.46 |
| Thermal diffusivity (cm2/s) | 0.44 |
| Vapor pressure (Pa) | 100 at 1050C 1 at 900 C |
| Elastic constants (Mb=1E12 dynes/cm2) at 300K c11, c12, c44 | 1.1810, 0.5320, 0.5940 |

Germanium

Properties of Ge

| Atoms/cm3 | 4.42E22 |
| --- | --- |
| Atomic Weight | 72.60 |
| Breakdown field (V/cm) | ~1E5 |
| Crystal structure | Diamond |
| Density (g/cm3) | 5.3267 |
| Dielectic Constant | 16.0 |
| Nc (cm-3) | 1.04E19 |
| Nv (cm-3) | 6.0E18 |
| Effective Mass, m*/m0 Electrons m*l m*l Holes m*eh m*hh | 1.64 0.082 0.044 0.28 |
| Electron affinity, x(V) | 4.0 |
| Energy gap (eV) at 300K | 0.66 |
| Intrinisic carrier conc. (cm-3) | 2.4E13 |
| Intrinsic Debye Length (um) | 0.68 |
| Intrinsic resistivity (-cm) | 47 |
| Lattice constant (A) | 5.64613 |
| Linear coefficient of thermal expansion, L/LT(C-1) | 5.8E-6 |
| Melting point (C) | 937 |
| Minority carrier lifetime (s) | 1E-3 |
| Mobility (drift) (cm2/V-8) | 3900 1900 |
| Optical-phonon energy (eV) | 0.037 |
| Phonon mean free path (A) | 105 |
| Specific heat (J/g C) | 0.31 |
| Thermal conductivity (W/cmC) | 0.6 |
| Thermal diffusivity (cm2/s) | 0.36 |
| Vapor pressure (Pa) | 1 at 1330C 1E-6 at 760 C |

# Indium phosphide

Indium phosphide (InP) is a binary semiconductor composed of indium and phosphorus. It has a face-centered cubic ("zincblende") crystal structure, identical to that of GaAs and most of the III-V semiconductors.

InP is used in high-power and high-frequency electronics because of its superior electron velocitywith respect to the more common semiconductors silicon and gallium arsenide. It also has a direct bandgap, making it useful for optoelectronics devices like laser diodes. InP is also used as a substrate for epitaxial indium gallium arsenide based opto-electronic devices.

Indium phosphide also has one of the longest-lived optical phonons of any compound with the zincblende crystal structure.[citation needed]

| Properties |
| --- |
| Molecular formula | InP |
| Molar mass | 145.792 g/mol |
| Appearance | black cubic crystals |
| Density | 4.81 g/cm3, solid |
| Melting point | 1062 °C (1335 K) |
| Solubility in water | slightly soluble in acids[1] |
| Band gap | 1.344 eV (300 K; direct) |
| Electron mobility | 5400 cm2/(V·s) (300 K) |
| Thermal conductivity | 0.68 W/(cm·K) (300 K) |
| Refractive index(nD) | 3.1 (infrared); 3.55 (632.8 nm)[2] |
| Structure |
| Crystal structure | Zinc blende |
| Coordination geometry | Tetrahedral |
| Thermochemistry |
| Std enthalpy of formationΔfHo298 | -88.7 kJ/mol |
| Standard molar entropy So298 | 59.8 J/(mol·K) |
| Specific heat capacity, C | 45.4 J/(mol·K)[3] |
| Hazards |
| MSDS | External MSDS |
| EU Index | Not listed |
| Main hazards | Toxic, hydrolysis to phosphine |
| Related compounds |
| Other anions | Indium nitride Indium arsenide Indium antimonide |
| Other cations | Aluminium phosphide Gallium phosphide |
| Related compounds | Indium gallium phosphide Aluminium gallium indium phosphide Gallium indium arsenide antimonide phosphide |
| (what is this?) (verify) Except where noted otherwise, data are given for materials in their standard state (at 25 °C, 100 kPa) |

# Electron affinity

The Electron affinity of a molecule or atom is the energy change when an electron is added to the neutral species to form a negative ion.

X + e− → X−

The electron affinity, Eea, is defined as positive when the resulting ion has a lower energy, i.e. it is an exothermic process that releases energy:

Eea = Einitial − Efinal

Alternately, electron affinity is often described as the amount of energy required to detach an electron from a singly charged negative ion[1], i.e. the energy change for the process

X− → X + e−

A molecule or atom that has a positive electron affinity is often called an electron acceptor and may undergo charge-transfer reactions.

## Electron affinities of the elements

Although Eea varies greatly across the periodic table, some patterns emerge. Generally, nonmetals have more positive Eea than metals. Atoms whose anions are more stable than neutral atoms have a greater Eea. Chlorine most strongly attracts extra electrons; mercury most weakly attracts an extra electron. The electron affinities of the noble gases have not been conclusively measured, so they may or may not have slightly negative EAs.

Eea generally increases across a period (row) in the periodic table. This is caused by the filling of the valence shell of the atom; a group 7A atom releases more energy than a group 1A atom on gaining an electron because it obtains a filled valence shell.

A trend of decreasing Eea going down the groups in the periodic table would be expected. The additional electron will be entering an orbital farther away from the nucleus, and thus would experience a lesser effective nuclear charge. However, a clear counterexample to this trend can be found in group 2A, and this trend only applies to group 1A atoms. Electron affinity follows the trend of electronegativity. Fluorine (F) has a higher electron affinity than oxygen and so on.

The following data are quoted in kJ/mol. Elements marked with an asterisk are expected to have electron affinities close to zero on quantum mechanical grounds. Elements marked with a dotted box are synthetically made elements—elements not found naturally in the environment.

| Group → | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ↓ Period |  |
| 1 | H 73 |  | He * |  |
| 2 | Li 60 | Be * |  | B 27 | C 122 | N * | O 141 | F 328 | Ne * |  |
| 3 | Na 53 | Mg * |  | Al 42 | Si 134 | P 72 | S 200 | Cl 349 | Ar * |  |
| 4 | K 48 | Ca 2 | Sc 18 | Ti 8 | V 51 | Cr 65 | Mn * | Fe 15 | Co 64 | Ni 112 | Cu 119 | Zn * | Ga 41 | Ge 119 | As 79 | Se 195 | Br 324 | Kr * |  |
| 5 | Rb 47 | Sr 5 | Y 30 | Zr 41 | Nb 86 | Mo 72 | Tc * | Ru 101 | Rh 110 | Pd 54 | Ag 126 | Cd * | In 39 | Sn 107 | Sb 101 | Te 190 | I 295 | Xe * |  |
| 6 | Cs 46 | Ba 14 | * http://en.wikipedia.org/wiki/Lanthanides | Hf | Ta 31 | W 79 | Re * | Os 104 | Ir 150 | Pt 205 | Au 223 | Hg * | Tl 36 | Pb 35 | Bi 91 | Po | At | Rn * |  |
| 7 | Fr | Ra | ** http://en.wikipedia.org/wiki/Actinides | Rf | Db | Sg | Bh | Hs | Mt | Ds | Rg | Cn | Uut | Uuq | Uup | Uuh | Uus | Uuo |  |
| * Lanthanides | La 45 | Ce 92 | Pr | Nd | Pm | Sm | Eu | Gd | Tb | Dy | Ho | Er | Tm 99 | Yb | Lu 33 |  |  |
| ** Actinides | Ac | Th | Pa | U | Np | Pu | Am | Cm | Bk | Cf | Es | Fm | Md | No | Lr |  |  |

| Chemical series of the periodic table |
| --- |
| Alkali metals | Alkaline earth metals | Lanthanides | Actinides | Transition metals |
| Poor metals | Metalloids | Nonmetals | Halogens | Noble gases |

## Molecular electron affinities

The electron affinity of molecules is a complicated function of their electronic structure. For instance the electron affinity for benzene is negative, as is that of naphthalene, while those of anthracene, phenanthrene and pyrene are positive. In silico experiments show that the electron affinity of hexacyanobenzene surpasses that of fullerene[2].

## Electron affinity of Surfaces

The electron affinity measured from a material's surface is a function of the bulk material as well as the surface condition. Often negative electron affinity is desired to obtain efficient cathodes that can supply electrons to the vacuum with little energy loss. The observed electron yield as a function of various parameters such as bias voltage or illumination conditions can be used to describe these structures with band diagrams in which EA is one parameter. For one illustration of the apparent effect of surface termination on electron emission, see Figure 3 inMarchywka Effect.